## Slide 1: Low Temperature Cure of PBO Films on Wafers
Bob Hubbard, Keith Hicks
Lambda Technologies, Inc.
Masayuki Ohe, Tomoko Kawamura
HD MicroSystems
Custom Polymer Design
Notes: 1
1

## Slide 2: Designing a Low-Temp Polymer
Increasing interest in low temperatures
  Moving to lower temperature sensitive devices (<200C)
  Need lower thermal budget for wafers & packages
  Need the same film properties (high Tg, elongation, etc.)
  Low stress and tailored mechanical properties
Recent progress
  150-200ºC polyimides (10th Symposium on Polymers)
  Lowered stress epoxies and silicones 2005
Polybenzoxazoles (PBO) wafer films
  Water processed
  Mechanical properties similar to polyimides
Notes: 2
2

## Slide 3: Limits to Convection Curing
Lower temperature curing compromises film properties
Polyimide convection limit appears to be around 250ºC
PBO convection limit appears to be 250-330ºC
Variable Frequency Microwave curing even lower
PI-2525

## Slide 4: Characteristics of VFM
Multiple frequencies excite a large number of modes resulting in a uniform energy distribution
Rapid frequency sweeping eliminates conditions that can cause arcing on metal components
Agile control and feedback for fast response
Benign process to semiconductors
  90 nm SRAM, DRAM, microprocessors, analog
  No change to device parameters or dopants

## Slide 5: Variable Frequency Microwaves
Multiple scanned frequencies
  4096 frequencies, each 260 Hz wide, for only 25 ms each
Dielectric relaxation causes dipole rotation
  Dipoles in uncured polymers cause whole chains to rotate
  Rotation of dipoles causes very efficient heating in bulk
C-band: 5.85-7.0 GHz
X-band: 7.9-8.7 GHz

## Slide 6: Compared with Fixed Microwave
Fixed Modes Create Hot Spots vs. Uniform Heating
Actual Results
Actual Results
Fixed Frequency
VFM

## Slide 7: Microwave Heating
Generates heat at the molecular level by forced oscillation of local molecular dipoles
A material’s ability to absorb microwave depends on:
-Each materials dielectric property
-Frequency of microwave energy
-Temperature of material
Heating is volumetric, throughout the material, as compared with external thermal transfer in convection heat
Convection Heat Microwave Heat
-Outside - In -Molecular level

## Slide 8: Material Interactions
  Glass &
  Ceramics
  Polymer
  resins
  Silicon
  Metals
Dp
~2 to 20 m
Dp
~2-50 m
Dp
~0.01 to 0.2 m
Dp
~0.1 to 2 m

## Slide 9: Dipoles in Polymer Resins
PI
BCB
PBO
Epoxies

## Slide 10: Polymerization Mechanisms
VFM ring closure reaction rate increase
polyimides (PI) polybenzoxazoles (PBO)
Faster, lower temperature polymerizations, cross-linking
C
O
O
H
H
N
C
N
O
C
O
O
H
Ar
H
C
N
O
C
O
Ar
C
O
N

## Slide 11: Previous Polyimide Results
A measure of microwave cure efficiency is the comparison of the final film Tg as cured conventionally and by VFM.
Example: convection cure at 4 hrs at 350ºC for Tg = 310ºC
VFM cure at 1.5 hrs at 150ºC for Tg = 310ºC
Tg Ratio = 1.0

## Slide 12: Electronic Correlations
While the dipoles involved in curing are absorbing microwave energy, there may be additional dipoles that are heating the molecule as well.
It is possible to calculate the total effective polarization of each structure by the matrix addition of the mean of each dipole contribution in each axis.
v1 = c11v1* + c21v2* + c31v3* + p11
v2 = c12v1* + c22v2* + c32v3* + p12
v3 = c13v1* + c23v2* + c33v3* + p13
> where each dipole is represented by vectors in the longitudinal (v1), transverse (v2), and vertical (v3) axes
> where C11 represents the cosine of the angle between each longitudinal vectors, for example
> where p11 represents the distance between the Cartesian coordinates of each vector

## Slide 13: Electronic Correlations
Dipole vectors used:

## Slide 14: Electronic Corellations
The molecular polarizabilities can be compared to the Tg just as other physical and optical properties are.
More examples are being added to clarify the relationship

## Slide 15: Structural Correlations
There is a well known correlation between a polymer’s “percent rigid chain length” (PRCL) and its physical properties including Tg.
The rigidity of a polymer resin backbone will inhibit its cure efficiency when exposed to microwave energy.
Apparently, there are additional factors

## Slide 16: Electronic and Structural Effects
Efficiency of microwave heating depends on:
  Number of dipoles available for microwave heating
    Dipoles involved in curing reactions
    Dipoles elsewhere in the molecules
  Structural flexibility (mobility of chain sections)
O
O
H
O
N
H
R
1
R
2
R
3

## Slide 17: Custom Design of PBOs
Crosslinking more complex than linear PI
Design options:
  Backbone: aromatic or alicyclic
  Chain endcap: dipole strength
  Cyclization promoter: yes or no
  Crosslinker: dipole strength
  Crosslinker: amount
Process options:
  Temperature of soak: 170-200ºC
  Time of soak: 1-2 hrs.
  Ramp rate up to soak: 0.2-1.0 deg/s
  Solvent: NMP or GBL
Design Matrix (DOE)
  Newly synthesized molecules
  Eight variables; 16 trials (28-5) with four center points
  Dipole strengths are not exact center points
Confirmation experiments and photolithography

## Slide 18: Cyclization Results
Model
  %Cycl. = 83.72 + 8.03 *AC + 7.46 *E + 6.69 *BG + 6.43 *G – 4.05 *D + 3.88 *DG – 3.83 *A
Backbone – Crosslinker Dipole interaction:
Endcap – Promoter interaction
Temperature

## Slide 19: Tg Results
Model
  Tg = 251.84 + 22.58 *E – 15.18 *DE – 11.10 *C + 10.89 *D + 6.94 *B - 5.33 *F + 4.92 *H + 3.44 *G
Temperature – Crosslink Amount interaction:
Crosslink dipole

## Slide 20: Other Properties
Residuals: Td(5%)
  Td5% = +381.48 +11.35 * A +41.57 * E +24.19 * G -23.08 * A * D +17.64 * B * G
  Backbone – Crosslink Amt interaction; Temperature; Promoter – Endcap interaction
Modulus
  Modulus = +2.58 +0.080 * A +0.35 * C -0.26 * E -0.22 * G -0.19 * A * C +0.21 * B * C
  Backbone – Crosslink Dipole interaction; Endcap – Crosslink Dipole interaction; Promoter; Temperature
CTE
  CTE = +63.41 -2.54 * A -1.33 * B -4.19 * D +2.98 * E +1.24 * G +2.72 * A * B
  Backbone – Endcap interaction; Crosslink Amt; Temperature
Elongation
  Elongation = +14.26 -9.27 * B +11.26 * E +8.73 * G -10.53 * H -7.37 * B * G
  Promoter – Endcap interaction; Temperature; Ramp Rate
Tensile Strength
  TS = +105.92 +8.08 * A -11.33 * B -7.36 * C -14.21 * E +21.52 * F +18.07 * G +5.77 * H -9.66 * A * B
  Backbone – Endcap interaction; Temperature; Time; Promoter

## Slide 21: Solvent Effects
NMP (N-methyl pyrolidone) was used for the primary experiment
GBL (g-butyrolactone) was used for a selected set of trials
Clearly NMP provides the highest cyclization, Tg, and lowest residuals.
 | Cycl % | elong | TS | Mod | Td5 | Tg | CTE
GBL | 53 | 8 | 127 | 2.98 | 257 | 257 | 57
(s) | 3 | 1 | 7 | 0.14 | 2 | 2 | 2
NMP | 89 | 11 | 110 | 2.57 | 421 | 280 | 57
(s) | 3 | 1 | 11 | 0.19 | 32 | 2 | 5

## Slide 22: Molecular Design
If the primary goals are highest cyclization and highest Tg:
  Use an alicyclic backbone and a crosslinking agent with a low dipole moment
    If an aromatic backbone is preferred, then use a high dipole agent
  Use a cyclization promoter and a low dipole endcap
    If a high dipole encap is used, the promoter doesn’t matter
  Use NMP solvent rather than GBL
To decrease the residual solvents and water in the film
  For an alicyclic backbone use low amount crosslinking agent
  For an aromatic backbone use high amount crosslinking agent
  Use a high dipole endcap with promoter
    OR a low dipole endcap with/without promoter
Note that Time and Temperature are relatively unimportant!

## Slide 23: Confirmation Runs
Results suggest confirmation runs:
Predicted results from the models:
Eighteen patterned wafers to determine effect on via slope (5 & 7 mm)
 | Backbone | Crosslink dipole | Crosslink amt. | Endcap dipole | Promoter
1 | Alicyclic | 6.53 | low | 2.66 | addn
2 | Aromatic | 7.56 | low | 2.66 | addn
3 | Aromatic | 7.56 | high | 2.66 | addn
Mtl-Temp | Cycl. % | Tg | Td5%
1-170C | 101.4 | 286.3 | 312.0
1-185C | 108.9 | 248.6 | 353.6
1-200C | 116.3 | 210.8 | 395.2
2-170C | 93.7 | 264.1 | 380.9
2-185C | 101.2 | 226.3 | 422.5
2-200C | 108.7 | 188.6 | 464.0
3-170C | 93.4 | 255.5 | 334.7
3-185C | 100.9 | 248.1 | 376.3
3-200C | 108.3 | 240.7 | 417.9

## Slide 24: Summary
PBO polymers can be custom synthesized for:
  Low temperature curing with VFM
  Unique mechanical properties
    As a result of the low temperature – fast cure
    As a result of the uniform bulk cure of VFM
Next steps
  Analysis of confirmation/photolithography runs
  Further refinement and selection of structures
  Feedback from users of PBO films for passivation and WLP
  Investigation of epoxy materials in progress

## Slide 25: 2007 Update on Patterned Wafers
Custom designed HD892X for VFM
  Confirmation runs led to more optimized formulation
  185°C full cure (Tg = 270°C)
  Elongation 70-80%, full adhesion, chemically resistant
  Smooth via profile from VFM processing
  Released for sampling to industry
oven cured VFM cured